## Slide 1
Bahgat Sammakia, Director and VP for Research
Benson Chan, Associate Director
Analytical and Diagnostics Laboratories
Jennifer Sammakia, Director
Tara Dhakal
Director
CASP
NSF I/UCRC
Kanad Ghose Director
ES2
Energy-Smart Electronic Systems
NSF Partnership for Industry
Mark Poliks Director
CAMM
Flexible Electronics
DoD Mfg. USA NYS CAT
CHIRP
Heterogeneous Integration
Bahgat Sammakia; Kanad Ghose; Ganesh Subbarayan (Purdue) Co-directors
SRC
SB Park Director
IEEC
Electronics Packaging
NYS CAT
Advanced Solar Energy

## Slide 2: Advance Packaging Design and Reliability at Binghamton University A New York State Center for Advanced Technology

## Slide 3: Resources / Facilities Smart Electronics Manufacturing Lab
MPM Momentum HiE Stencil Printer
EKRA Serio 4000 Stencil Printer
Koh Young Solder Paste Inspection
Universal Fuzion Pick and Place (CAMM)
Universal High Speed Wafer Feeder (CAMM)
Fine Tech Pico Ma (manual bonding/component placement (CAMM)
Heller 1707W Reflow Oven
Koh Young Automated Optical Inspection
Fuji Placement tool
PVA Conformal Coating / Underfill
Koh Young Automated Optical Inspection
Koh Young Meister – conformal coat and underfill inspection

## Slide 4: Resources / Facilities Smart Electronics Manufacturing Lab
MPM Momentum HiE Stencil Printer
EKRA Serio 4000 Stencil Printer
Koh Young Solder Paste Inspection
Universal Fuzion Pick and Place
Universal High Speed Wafer Feeder
Heller 1707W Reflow Oven
Koh Young Automated Optical Inspection
Fuji Placement tool
PVA Conformal Coating / Underfill
Koh Young Automated Optical Inspection
Koh Young Meister – conformal coat and underfill inspection

## Slide 5: Advance Packaging – IEEC
Provides expertise in:
  Environmental and Reliability testing, test vehicle design, build and data analysis
  Teardown analysis, construction analysis, understand latest trends in packaging
  Failure analysis, root cause, analytical and diagnostic tools
  Mechanical and thermal modeling, warpage understanding and control, large body sizes
  Materials characterization, interactions

## Slide 6: Warpage Control for Advance Packaging

## Slide 7: 2.5D Package Development
AMD Fiji Package
Large Graphics Processor
(4x) High Bandwidth Memory (HBM, 4 die stack)
Mechanical Modeling
Thermal Modeling
Model verification using Digital Image Correlation (DIC)
Materials evaluation
Assembly process development, assembly order

## Slide 8: 2.5D Warpage Studies
In most packaging architectures, manufacturing steps occur at elevated temperatures when the assembly is nearly plat. As cooling takes place, out-of plane deformation can occur due to CTE mismatches.
  Non-uniform expansion/contraction of die and substrate in temperature cycle.
  Results in warpage of the package which is major reliability concern.

## Slide 9: Wafer Warpage During Reflow
300 mm fully defined and back ground wafer processed in a reflow cycle from 25 °C to 240 °C
Digital Image Correlation (DIC) warpage measurement was measured through the simulated reflow temperature cycling

## Slide 10: Failure Isolation and Analysis of a Functional Circuit Board

## Slide 11: Background
A populated printed circuit board was returned to a client
  This was an impedance test fail on a populated board
  Labeled as an “open” trace
  NOTE: “open” means out of spec high, in this case “open” was an Ohm or two
Two objectives to be met
  Isolate the failure
  Determine the cause of the failure
  To facilitate failure isolation, the client provide circuit design for the affected area
General area of the defect(s)

## Slide 12: Routing of the Trace in Question
Pen marking shows the routing of the circuit line, which was all on one internal layer

## Slide 13: Exposing Probe Points in the Board
1
4
3
2
Pits were dug down to, and beyond the plane of the affected circuit line – traces were exposed to allow probing
  1st was in the center (1)
    High resistance remained between the center and the left and right ends
  2nd set (2 and 3) was dug between the center and ends
    High resistance remained between 2 and the left end, and between 3 and the right end
    Continuity was observed between 1 and 2 and between 1 and 3
  Last pit (4) was dug between the left end and location 2
    Continuity was observed between 2 and 4
    High resistance was found between 4 and the left end

## Slide 14: Final Analysis of the Failure
Final isolation
  The left section was excised from the board
  Flat sectioned to the layer in question
  The flat section expose additional areas that could be used as probe points (a, b, and c)
Probe results
  Continuity between a and b
  High resistance between b and c
Flat sectioned
c
a
b

## Slide 15: Conclusion
Fine dark line around the edge of the pad
  This is drill smear
  The plated via does not fully contact the pad
  This accounts for the high resistance reading
  Some contact affords continuity but not to a low enough resistance
Other pads in the flat section showed drill smear
  In this case, pass/fail is a matter of degree
  Other pads had sufficient contact with the via to allow acceptable trace continuity

## Slide 16: Joining Metallurgy Characterization between M1 chip and Si Bridge in Apple M1 Ultra Package

## Slide 17: Apple Mac Studio Ultra
70mm Package
Silicon bridge connection

## Slide 19: Joining metallurgy between Apple Ultra M1 logic chip and Si bridge
M1 chip circuits
Si bridge circuits
Core Substrate w/ embedded device

## Slide 20: Joining metallurgy between Apple Ultra M1 logic chip and Si bridge
M1 chip circuits
Cu bump
Si bridge circuits
Cu bump
Sn
Aluminum final metallization
Polyimide
Underfill 1
The second cu bump is made to enhance the strength of the interconnect, compare to solder on flat, the solder is able to have more surface area. The top bump is also 10% larger than the bottom to better distribute stress
25 micron pitch

## Slide 21: Joining metallurgy between Apple Ultra M1 logic chip and Si bridge
M1 chip circuits
Cu bump
Si bridge circuits
C4 Bumps
Aluminum final metallization
RDL
Underfill 2
Through Mold Via

## Slide 22: Joining metallurgy between Apple Ultra M1 logic chip and Si bridge
M1 chip circuits
Cu bump
RDL
Cu bump
Aluminum final metallization
Polyimide
EMC 1
Thru mold vias (outside of bridge region)

## Slide 23: Overall cross section showing Si bridge, substrate, BGA, and PCB
PCB board cross section
Substrate cross section
BGA
C4 (flip chip joining)
Micro bump joining for M1 and Si bridge

## Slide 24: Overall cross section showing Si bridge and substrate at higher magnification
Cu Bump M1 chip
Micro joining metallurgy
Si bridge
Underfill 1
Molding compound
Underfill 2
Solder mask
8-2-8 Substrate
Backside grinding plane
3 layer RDL
C4 bump

## Slide 25: A cross section of Si Bridge and substrate Interface edge
Substrate
C4 (flip chip joining, not shown here)
Micro bump joining for M1 and Si bridge
PSPI and wiring
Underfill 1 (for micro joining)
Underfill 2
Solder masks
Molding compound
Si bridge diced edge
Backside grinding plane
PSPI and wiring levels formed after backside grinding
Underfill Fillet

## Slide 26: Micro bump pitch of Si bridge joining metallurgy
Measurements showing about 25 micron bump pitch for both M1 and Si bridge.

## Slide 27: M1 Ultra packaging “thought” assembly process (tentative)
M1 chip wafer finishing and bump formation
Si bridge wafer finishing and bump formation
Dicing for singulation
D2D attach by micro bump joining
Underfill 1 for micro bump joining
Thinning Si bridge sides of molded wafers
Build up Cu wire/PSPI layer
C4 solder bumping
8-2-8 substrate
M1 backside thinning
Dicing for singulation
Chip joining by reflow
M1+M1+ Si bridge subassembly
Underfill 2 for C4
PCB main board
BGA attach
Assembly refow
Singulation mechanical dicing and reconstitute to a wafer (2 M1 dies very accurately)

## Slide 28: Copper Hybrid Bonding – AMD Ryzen 7 5800X3D

## Slide 29
Source: Binghamton University & Prismark Partners
Die Stacking in AMD Ryzen 7 5800X3D
16 um
1.6 um dia
Direct Copper to Copper Bond: ~1.6 um dia columns on 15.5 um pitch
Stacked L3 cache
Source: AMD

## Slide 30: Apple iPhone 16Pro Camera module, CuCu Hybrid Bonding

## Slide 31: Camera Module 2 Cross Sections
IR Filter
Sensor
Interconnect
Camera Image Sensor

## Slide 32: Camera Module 2 Cross Sections
IR Filter
Sensor
Interconnect
Camera Image Sensor

## Slide 33: Camera Module 2 Cross Sections
Lens Stack
IR Filter
Camera Sensor

## Slide 34: Camera Module 2 Cross Sections
Lens Stack
IR Filter
Camera Sensor

## Slide 35: Camera Module 2 Cross Sections

## Slide 36: Camera Module 2 Cross Sections

## Slide 37: Camera Module 2 Cross Sections