## Slide 1: Enabling hybrid and additive approaches to medical and industrial devices Mark D. Poliks SUNY Distinguished Professor Empire Innovation Professor Director, Center for Advanced Microelectronics Manufacturing A New York State Center of Advanced Technology New York Node, NextFlex Manufacturing USA Binghamton University, State University of New York mpoliks@binghamton.edu 607-727-7104 (mobile)
1

## Slide 2: S3IP Organization Chart
Analytical and Diagnostics Laboratory
Dr. Bahgat Sammakia, Director and VP for Research
Mr. Benson Chan, Associate Director
Dr. Jenny Sammakia, Director
Binghamton University Faculty & Students
COE
NECCES
Advanced Batteries
DoE EFRC
NSF Engine, etc.
CASP
Advanced Solar Energy
NSF Early Career
IEEC
NYS CAT
Electronics Packaging
CAMM
DoD Manufacturing USA
Flexible Electronics
NSF I/UCRC
ES2
Energy-Smart Electronic Systems
CHIRP
Heterogeneous Integration
SRC
Prof. Stan Whittingham Director
Prof. Tara Dhakal
Director
Prof. Mark Poliks Director
Prof. SB Park Director
Prof. Bahgat Sammakia; Prof. Kanad Ghose; Prof. Ganesh Subbarayan (Purdue), Co-directors
Prof. Kanad Ghose Director
NYS CAT

## Slide 3: Center for Advanced Microelectronics Manufacturing
CAMM was founded in 2005 with funds from NYS and ARL
A New York State Center of Advanced Technology (CAT)
New York Node NextFlex Manufacturing USA
Specialized facilities for large panel, roll-to-roll, printed and component assembly, fabrication and test
~10-15 unique projects at a given time
Support company (and academic) related R&D programs
Technical staff of five, plus graduate students working on funded projects, also, in part, operate as a user facility
Host three companies within CAMM facilities
Funded by company, federal, and NYS (CAT), responsible for economic development in NYS
Approximately 10K sq ft of class 1000 capable cleanroom space located at the Huron Campus, Endicott NY (former IBM site). More than 30K sq ft in three locations
In addition: S3IP NYS Center of Excellence affiliated supporting facilities and centers (IEEC, SRC-CHIRP, ES2, ADL, NLab, etc.)

## Slide 4
Other CAMM and S3IP Facilities and Equipment
Roll-to-Roll Manufacturing Facilities:
Lithography
Vacuum Sputter Deposition (KDF, GVE, and CHA)
Handling, Inspection, Lamination, and Wet Processing
Characterization:
Keyence VK-X1050 laser scanning confocal microscope
VHX-6000 digital microscope
RF vector network analyzers up to 40 GHz
LCR meters and data acquisitions units
Netzsch DEA 288 Dielectric Analyzer
High precision electrical resistance meters, source meters, and power supplies
Other equipment:
Novacentrix PulseForge Invent photonic curing
Atmospheric plasma jet-flow system for surface modification
Contact angle measurement (goniometer)
Dremel Digilab LC40 laser cutter
FinTech Pico pick and place
Rheomter and viscometer
Other S3IP Facilities & Equipment
Analytical and Diagnostics Lab (ADL)
  SEMS/ TEM / FIB
  IR microscope
  X-ray, CT scan, and CSAM
  Materials and element analysis equipment (XPS, EDX, FRIR,…)
  Thermal suite includes DSC, TGA and TGA/MS,…
IEEC , Failure Analysis and Reliability Lab
The Nanofabrication Lab

## Slide 5
Understand the challenges to interface thin, hard and soft electronic components – neutral axis engineering
Heterogeneous device Integration
Thinned semiconductor device handling, placement, assembly, anisotropic conductive adhesives
Printing, patterning, conductive inks & sintering
Sustainable materials and fabrication processes
Interconnecting in the z-direction: printed vias
Additive manufacturing of resistors, capacitors, inductors & interconnects
Stretchable & highly stretchable conductive inks
Printed RF components design & fabrication, interconnects and high-temperature applications
Wearable medical devices
  Multilayer printed & laminated structures
  Sweat and hydration patch – microfluidic channels & printed electrochemical sensors
  Vital signs patch for ambulatory aeromedical care
Planar SiC high-power module packaging with printed interconnections
Electromechanical, RF, temperature/humidity, power cycling testing and reliability studies
Flexible, Hybrid & Additive

## Slide 6
Silver Via on PI
Au on Ceramic
Au on 40µm Ceramic
CNS on PET
Photoresist on FR4
Ag & dielectric on LCP
Platinum on Ceramic
Silver on Paper
Dielectric and Au on Ceramic
Silver on PI
Multilayers Leadset
Large Area Printed Sensors
Confocal Printing
Substantial printing equipment including AJP 5X and 3X, stencil/screen printers, dispensers, and inkjet printers
Laser sintering module (up to 40W) with reducing gas environment and UV curing module as well.
Demonstrated printing different inks on many substrates in planar and 3D complex irregular substrates
PulseForge Invent photonic sintering, convection ovens, high temp furnaces, UV expose, laser cutting etc
Example of Facilities: Additive Manufacturing -- Printing and Processing

## Slide 7: XTPL Ultra-Precise Printing
XTPL _ Delta Printing System
High resolution printing method.
Combines high-precision pressure control and axes.
Flexible glass capillary tips.
Ink: Heraeus RP Au 041008/HT (high temperature Au ink)
XTPL Printer at CAMM
X-axis camera
Y-axis camera
Light
Light
Flexible glass capillary tip
High-precision pressure inlet
XTPL Printhead Schematic
3 mm
0.5 mm
Design-01
Characterization:
0.5 mm
Printed Traces Conductivity
Average conductivity 2.7X10^7 S/m
67.5% of bulk gold
50X Magnification
Trace profile
Design-02
SEM of gold particle free ink after firing (15K Mag.)
Firing:
Drying the printed samples in the box oven at 90°C for 15 mins.
Firing the samples at 850°C for 10 mins in high temperature furnace.
15K Mag.
Notes: - High-resolution printing method ∼ 1µm to nano printing.
- Ink: high-mass loading, small particle size and high viscosity.
- Developing high-temperature and embedded electronics, especially in aerospace applications.
- Using XTPL technology could drive advancements in microelectronics industry.

## Slide 8: Progress In Advanced Printing Technologies (Micro Dispensing)
Łysień, Mateusz, et al. "High-resolution deposition of conductive and insulating materials at micrometer scale on complex substrates." Scientific Reports 12.1 (2022): 9327.
XTPL® Delta Printing System
Micro AM 3D printer that uses Ultra Precision Deposition (UPD) technology

## Slide 9
Ink Continuity and Printing Interconnects on Irregular Surfaces (2/2)
Printing on Si Dies
The interconnects were printed from the Si die into the PET substrate.
200 μm diameter pads (25 nos.) and 300 μm ones (12 nos.) were printed to investigate the footprint area that can be obtained on 3x3 mm Si die
3X3mm Si die
NEA123
Printed Ag ink
NEA123
Printed Ag ink
3X3mm Si die
25 pads (200μm)
12 pads (300μm)
300μm pads
200μm pads
Printed daisy chain between dog bone pads on Si die and PET substrate
A daisy chain was printed to link several test pads in a sequential chain.
The average resistance at different sides of the daisy chain is 32.4 Ω, which demonstrates the stability of printed silver particle-free ink over irregular objects.
0.380 µm lines thickness
Printing with 3 layers
Cured at 140°C for 1 hr.
35 µm wide circuit lines are 5-7 ohms

## Slide 10: Vital Signs Patch
  -Continuous wireless vital signs sensing for up to 1 week (Clinical grade)
  3-Lead ECG, Respiration, Reflective PPG, Core Body / Skin Temperature, Accelerometer
  - End-to-end prototype manufacturing & supply chain development
  Disposable devices
  - Algorithms
  Android UI, Decision Making, CNIBP
  -On-demand wireless minimally invasive measurement of metabolites, proteins and hormone concentrations
  Lactate, cytokines, catecholamines. Patch actuation
  -End-to-end prototype manufacturing & supply chain development
  Reusable electronics unit & disposable sensors
  - Algorithms
  Android UI
Interstitial Fluid Patch
  - Continuous wireless hydration sensing during moderate/intense exercise for up to 24 hours
  Electrolytes (Na, K), Sweat rate
  -End-to-end prototype manufacturing & supply chain development
  Reusable electronics unit & disposable sensors
  - Algorithms
  Android UI
Sweat Hydration Patch

## Slide 11: Human Subject Testing
Patient Monitoring at Home:
Prediction and Prognosis of Infectious Diseases
Hydration Status & Heat Stress Assessment
Partnerships
Synergistic Activities
DARPA MBA (GE): Performance & Aptitude Assessment & Human Subject Studies at West Point
From the Lab to Manufacturing Supply Chain to End-users
Ambulatory Patient Monitoring & En-Route Care
Image courtesy of AFRL
Image courtesy of AFRL
Continuum of care

## Slide 12
A broadband antenna for 2.4GHz was fabricated using suitable materials found to sustain 750°C.
Interrogation of printed antenna array embedded into fiberglass composite during mechanical testing
S-parameters measurements of printed gold transmission lines onto 3D printed ceramic up to 750 °C
Inverted F-Antenna
Microstrip Lines
12 GHz phase array
Design Tools
  ANSYS High-frequency structure simulator (HFSS)
  Advanced Design System (ADS)
RF vector network analyzers up to 40 GHz with various RF probes and horn antennas, test chamber
Substantial experience in understanding the effect of printing method, inks, substrates, postprocessing, and mechanical and environmental stress on RF performance
RF Design, Modeling/Simulation, and Test
Various RF components AJP printed on PI
Stretchable Microstrip line w/ vias, printed with Liquid Metal
IJP patch antenna during bending

## Slide 13
You are invited to join us!
Keynote lecture
Poster session
Reception
& more

## Slide 14
Join us for the 36th Annual Electronics Packaging Symposium
at the GE Research (Aerospace) Campus!

## Slide 15
CAMM Research Partners
Organic Robotics Corporation