## Slide 1: 3D Interconnections from Solder Balls to Hybrid Bonding
Transient Liquid Phase (TLP) Bonding
> 100 mm | 40 – 20 mm | 20 – 10 mm | < 10 mm | < 1 mm (for AI chips)
Flip chip: solder Bumps | Microbumps Cu pillars with solders | Transient Liquid Phase1 Cu-Cu bonding2 | Solderless Cu-pillar1 Hybrid bonding (Cu/SiO2)2 | Hybrid bonding (Cu/SiO2) and beyond
Solder Reflow | Solder Reflow | 1Low-pressure, annealing 2Thermo-compression | 1Thermo-compression 2Two-step: comp. & anneal. | Two-step: compression & annealing
Underfill | Underfill | Underfill | Underfill/No underfill | No underfill
Interconnect pitch spacing (pad-pad, via-via)
Cu Pillar/Solder
Reflowed at 260 °C
Cu-Cu Thermo-compression Bonding (W2W)
Fine-pitch scaling
Ultrafine-pitch scaling
Hybrid Bonding (D2D)
(IBM test chips)